## Slide 1: PREPARATION AND CHARACTERIZATION OF PHOTON UPCONVERTING CATALYSTS FOR PHOTO WATER SPILTTING HYDROGEN PRODUCTION.
Asitha U. Malikaramage,
University of Peradeniya,
Peradeniya,
Sri Lanka.

## Slide 2: What is Water splitting ?
Highly endothermic process; ΔH > 0
“Thermodynamically Uphill” reaction
Semiconductors are used as light harvesters

## Slide 3: Band-gap Requirement for water photo-splitting:
Notes: A photo catalytic water splitting reaction over a semiconductor material

## Slide 4: Common Semiconductors:
SrTiO3
3.2 eV
Lower edge position of the conduction band
Upper edge position of the valence band

## Slide 5: Photon Upconversion and Localized Surface Plasmon Resonance (LSPR) in photo water splitting
Schematic diagram of photon upconversion phenomina
Proposed photocatalytic process for efficient hydrogen generation
using the Ag- TiO2 nanostructures, based on excitation of the LSPR
under visible-light and infrared irradiation

## Slide 6: Synthesis
Preparation of UCM
TTIP + IrCl3 + Ag(NO3) +Ethanol
+Glacial Acetic acid
Sol gel
Autoclaved the mixture in 150ºC for 2 hours and dried the sample in vacuumed oven at 100 ºC
Mixed and stirred for 30 min and adjust the PH value for 3-5 using conc. Diluted KOH
Refluxed at 200 ºc for 48 hours using a mixture of diethelene glycole and hexane as the solvent (

## Slide 7: Characterization
XRF data

## Slide 8
XRD data
IrO2 phase
TiO2 phase (Anatase form)

## Slide 9
AgO phase
Ag phase

## Slide 10
Figure 03 . SEM images of Ag/Ir doped TiO2 nanoparticles
SEM Images
Non sintered
Sintered

## Slide 11: UV-visible absorbance spectra
Figure 04 . UV –visible absorbance spectra for the sample

## Slide 12: FTIR spectroscopy
Figure 05. FTIR spectroscopy
huge peak around 600 cm-1 typically it represents the Ti-O-Ti bonds and Metal attachments to the Ti atom. So this can be used as a confirmation of Ti-Ir and Ti-O-Ir bonding.

## Slide 13
Video 01: Photo water splitting under 1 sun
When only distilled water used to produce the hydrogen and oxygen . Efficiency of hydrogen production reduced with time. (5 mins).
To overcome this problem Ethanol was introduced as a scarifying agent .
So this can be also used to degrade organic pollutants to smaller molecules (CO2 , CH2O,…ect)
2h+ + C2H5OH / 2H+ + CH3CHO

## Slide 14: Conclusions
Iridium / silver nano-composite can be used as an efficient photo water splitting material.
The material can be used to degrade organic pollutants in water in favorable of purifying water.

## Slide 15: Future works
To measure the hydrogen evolution rate from the GC –TCD technology
Get TEM images of the material.
Do the further characterization of new hydrothermally grown nanorods /nanoflowers assisted water splitting material.
Introduce Holmium , Samarium and Gadolinium to the material.

## Slide 16: Thank you !!